### STRUCTURAL GENERAL PURPOSE

### ADHESIVE/SEALANT – VERY HIGH GRAB VERSION

#### S - 732 U VHG

# OVERVIEW

Manufactured by Structural Adhesives Ltd, S-732 U VHG is a high grab adhesive which is more flexible than Epoxy based adhesives and is a non-hazardous single part formulation.  This adhesive will take up some movement.

#### DESCRIPTION

S - 732 U VHG is a high quality, neutral, elastic one component construction joint sealant and universal adhesive based on a hybrid polymer. The Very High grab version is formulated for brick slip bonding in situations where extremely good grab is required i.e. in the soffit of an arch.

# Characteristics

- Very easy application

- Excellent adhesion on many surfaces

- Stays permanently elastic after curing

- Does not smell

- Can be painted ‘wet on wet’

- Excellent weather resistance

- Resistance to many chemicals does not stain on porous surfaces such as natural stone blue stone, marble, granite

- May be applied on wet substrates

## Applications

- Sealing and bonding in the building and metal industry

- Structural bonding in vibrating constructions

- Fixes almost any material to almost any substrates

## Application Examples

Sealing of floor joints

Connection joints between metals

Supple bonding in shipbuilding, car body and container industry

Bonding of wall panels

Joints between precious natural stones such as numerable

Glues almost any material onto any substrates

###### Technical Specification

| Curing System: | Moisture cures |
| --- | --- |
| Skin formation : | ca 10 min (20° C /65% R.H) |
| Curing Rate: | 2 mm /24h (20° / 65% R.H) |
| Hardness : | 60+5 shore A |
| Shrinkage: | None |
| Specific Gravity: | 1.53 |
| Temperature Resistance : | -40°C to +100° C |
| Elongation at break: | 300 % (DIN 53504) |
| Elasticity Modulus 100%: | 1.35N/mm2 (DIN 53504) |
| Tensile Strength: | 2.20 N/mm2 (DIN 53504) |
| Maximum allowed distortion: | 25% |

## Chemical Resistance: -

| Good against: | Salt Water |
| --- | --- |
|  | Aliphatic Solvents |
|  | Diluted inorganic acids and alkalis |
|  | Mineral oils |
|  | Grease |
| Does not resist: | Aromatic Solvent |
|  | Concrete Acid |
|  | Chlorinated Hydrocarbons |

## Surfaces

S-732 U VHG adheres to all usual building substrates treated wood, PVC metals and many plastics. All surfaces must be clean and free from dust and grease.  Surfaces may be humid.

Not suitable for: PE, PP, Teflon, wax, neoprene and bituminous surfaces.

## Preparation

A primer should be applied to very porous surfaces.  No pre-treatment is necessary to non-porous surfaces.

## Application

| Application Method | Manual or pneumatic caulking gun. |
| --- | --- |
| Application Temperature | +1°C to + 30°C |
| Tool With | Soapy solution before skin forming |
| Repair with | S-732 U VHG |

## Coverage

A 290cm³ cartridge applied in a 5mm bead, 2 beads horizontally per brick slip will give coverage of approximately ½m².

## Special Comments

S-732 U VHG may be overprinted, however due to the large spectrum of paints and varnishes strongly suggest a compatibility test best application.  When overprinted with paints based on alkyd resins drying time of the paint may increase.

The above figures do not constitute a specification.  They represent typical values obtained for this product.

## Health and Safety

Before using this product ensure that you have been supplied with and have read carefully the following information.

- The hazard label (complying with CHIP Regulations 1995) applied to the container.

- Structural Adhesives Material Safety Data Sheet S-732 U VHG.

## Packaging

S-732 U VHG is supplied in a 290ml cartridge, in boxes of 12. This would give 6m2 of coverage as a guide.

## Storage

S-732 U VHG should be stored in unopened packaging in a dry and cool place.

NOTE

This disclaimer is issued by Structural Adhesives Limited ("the Company") and applies to the use of any products supplied by the Company ("the Products") displayed on this Technical Data Sheet (“TDS”). Please read this disclaimer carefully before using any of the Products. While the information and recommendations in this publication are to the best of our knowledge, information and belief, accurate at the date of publication, Structural Adhesives Ltd MAKES NO WARRANTIES, EXPRESSED OR IMPLIED OR OTHERWISE.  IN ALL CASES THE USER IS RESPONSIBLE FOR DETERMINING WHETHER THE STRUCTURAL ADHESIVE LTD PRODUCT IS FIT FOR A PARTICULAR PURPOSE AND SUITABLE FOR USER'S METHOD OF USE OR APPLICATION. THE PRODUCT MAY PRESENT HAZARDS AND SHOULD BE USED WITH CAUTION.  WHILE CERTAIN HAZARDS ARE DESCRIBED IN THIS PUBLICATION, NO GUARANTEE IS MADE THAT THESE ARE THE ONLY HAZARDS THAT EXIST.  Hazards, toxicity and behaviour of the products may differ when used with other materials and are dependent upon the manufacturing circumstances or other processes.  It is essential that the user evaluate hazards, toxicity and behaviour and this information be made available to processors, handlers and end users.

Using this TDS and/or the product constitutes your acceptance of this disclaimer.  This TDS covers just one of a large range of products supplied by Structural Adhesives Ltd.

Full information on these products and advice on application is freely available from our fully trained technical team. However NO PERSON OR ORGANISATION EXCEPT A DULY AUTHORISED STRUCTURAL ADHESIVES LTD EMPLOYEE IS AUTHORISED TO MAKE AVAILABLE DATA SHEETS FOR STRUCTURAL ADHESIVES LTD PRODUCTS.  DATA SHEETS FROM UNAUTHORISED SOURCES MAY CONTAIN INFORMATION THAT IS NO LONGER CURRENT OR ACCURATE.

This TDS supersedes all previous TDS’s relating to the products, and users of it must ensure that it is the current issue. Destroy all previous TDS’s, and if in any doubt, contact Structural Adhesives Ltd quoting the product and data sheet number.

No part of this data sheet can be reproduced or transmitted in any form, or by any means without prior written consent from Structural Adhesives Ltd.

This product is further sold subject to the Company's Conditions of Sale, which are made available to the customer prior to an order being accepted.